## Slide 1
B.Sc. Thesis Defense • CE 400 • September 2026
Comparative Analysis of Locally Produced Bitumen and Imported Low-Cost Bitumen for Bangladesh Road Construction
Focusing on Aggregate Shape
Md Rakibul Hasan Mridha (2020333545) • Md Sagor Hossain Saddas (2020333553)
Supervisor: Prof. Md Johir Bin Alam, Dept. of CEE, SUST Co-Supervisor: Mohiuddin Arif, Lecturer, Dept. of CE, SEC
Department of Civil Engineering • Sylhet Engineering College • SUST, Sylhet-3100
1/16

## Slide 2
PRESENTATION OUTLINE
01
Background & Problem Statement
02
Objectives of the Study
03
Methodology & Experimental Design
04
Results — Aggregate & Bitumen Properties
05
Results — Marshall Mix Design & OBC
06
Results — Comparative Analysis of Mixes
07
Proposed Roadmap for Bangladesh
08
Conclusions & Future Work
09
References
2/16

## Slide 3
BACKGROUND & PROBLEM STATEMENT
375,000 km
Road Network in Bangladesh
>90%
Flexible Pavements
92–96%
Aggregate in HMA by Weight
Tk 6,300
ERL Bitumen Price/Unit
The Problem
▸ Imported bitumen shows inconsistent penetration grades and rheological properties [2]
▸ Premature pavement distresses: rutting, stripping during monsoon, fatigue cracking [4]
▸ RHD has restricted certain imported grades due to quality concerns [2]
▸ Most research treats bitumen quality and aggregate shape as separate variables [7]
▸ No systematic combined study under Bangladesh's subtropical monsoon conditions
Research Gap
▸ Cubical aggregate effects studied separately [3, 5]
▸ Subgrade stabilization studied in isolation [7]
▸ No one has examined how aggregate shape + bitumen source quality interact in Bangladesh
▸ No systematic comparison of local ERL vs imported 60/70 binder with 20% cubical replacement
▸ This study fills that gap with side-by-side comparison
3/16

## Slide 4
OBJECTIVES OF THE STUDY
i.
Compare physical properties (penetration, softening point, ductility, specific gravity, flash & fire point) of local and imported 60/70 bitumen.
ii.
Determine the Optimum Binder Content (OBC) using the Marshall method for the control mix with local bitumen.
iii.
Evaluate the effect of cubical aggregate shape (20% replacement of coarse fraction) on Marshall mix design properties.
iv.
Assess the performance of four mix combinations in terms of Marshall stability, flow, and volumetric properties.
v.
Compare the four mixes in terms of required pavement thickness, cost effectiveness, and load bearing capacity.
vi.
Provide practical recommendations for material selection in Bangladesh's road construction practice.
4/16

## Slide 5
METHODOLOGY
Experimental Design & Testing Programme
Materials
▸ Local ERL Bitumen (60/70 grade)
▸ Imported Low-Cost Bitumen (60/70 grade)
▸ Crushed Stone Aggregates — Sylhet Quarry
▸ Stone Dust as Mineral Filler (passing 0.075 mm)
▸ NMAS: 19 mm (DBM Grading-II, MoRTH Table 500-10)
Mix Design Matrix
Mix-1
Local + Natural Agg.
Control + OBC
Mix-2
Imported + Natural Agg.
Imported Control
Mix-3
Local + 20% Cubical
Shape Effect (Local)
Mix-4
Imported + 20% Cubical
Shape Effect (Imp.)
Testing Programme
▸ Marshall Stability & Flow (ASTM D6927)
▸ Volumetric Analysis (Va, VMA, VFB)
▸ OBC from 5 trial binder contents (4.0–6.0%)
▸ 75 blows/face — Heavy traffic spec
▸ 60°C water bath, 30–40 min conditioning
▸ 12 specimens total across 4 variants
5/16

## Slide 6
AGGREGATE SHAPE CLASSIFICATION
Zingg Diagram Method for Coarse Aggregates (19–12.5 mm)
Zingg Classification System
Shape
Elongation (dI/dL)
Flatness (dS/dI)
Blade
< 2/3
< 2/3
Rod
< 2/3
≥ 2/3
Disc
≥ 2/3
< 2/3
Cubical ✓
≥ 2/3
≥ 2/3
Elongation Ratio = dI / dL Flatness Ratio = dS / dI
dL = longest, dI = intermediate, dS = shortest dimension Measured with Vernier calipers on retained 12.5 mm fraction
Why Cubical Aggregates?
▸ Better mechanical interlock between particles [3, 4]
▸ Higher internal friction → more rutting resistance [5]
▸ Flaky/elongated particles break under traffic loading [4]
▸ 20% cubical replacement — based on Teja & Krishna (2020) [3]
▸ Aggregate shape affects compaction, stability, and deformation [6, 8]
Approach: Cubical particles hand-sorted and used as 20% replacement of coarse aggregate (Material A) by weight in Mix-3 and Mix-4.
6/16

## Slide 7
RESULTS — AGGREGATE PROPERTIES
Physical & Mechanical Properties of Sylhet Quarry Aggregates
Property
Result
Spec. Limit
Standard
Status
Aggregate Impact Value (AIV)
18%
≤ 27%
IS 2386 Part IV
✓ PASS
Aggregate Crushing Value (ACV)
20%
≤ 30%
IS 2386 Part IV
✓ PASS
Flakiness Index
15%
≤ 30%
IS 2386 Part I
✓ PASS
Elongation Index
23%
≤ 30%
IS 2386 Part I
✓ PASS
Los Angeles Abrasion
—
≤ 30%
ASTM C131
✓ PASS
Water Absorption
—
≤ 2%
ASTM C127
✓ PASS
Specific Gravity (Coarse)
—
2.5–2.9
ASTM C127
✓ PASS
All aggregate properties met the specification requirements — suitable for Dense Bituminous Macadam (DBM) mix design.
7/16

## Slide 8
RESULTS — BITUMEN PROPERTIES
Local ERL vs Imported Low-Cost Bitumen (60/70 Grade)
Penetration
64 vs 68
dmm at 25°C
Both within 60–70
Softening Pt.
52 vs 41°C
Ring & Ball
Imported FAILS spec
Ductility
112 vs 91 cm
at 25°C
Imported borderline
Flash Point
255 vs 218°C
Cleveland Open Cup
Imported FAILS spec
Sp. Gravity
1.023 vs 0.99
at 25°C
Imported below range
Regional Comparative Assessment — South Asia
▸ Local ERL bitumen passes ALL regional specifications — Bangladesh RHD, India MORT&H, Nepal DOR, Pakistan NHA
▸ Imported bitumen's softening point (41°C) falls below minimum of all South Asian authorities (47–48°C min)
▸ Imported flash point (218°C) fails the 232°C safety threshold used across the region
▸ Imported specific gravity (0.990) below the 1.01–1.06 range required by regional standards
▸ Conclusion: Imported bitumen tested does NOT meet regional specifications for flexible pavements
8/16

## Slide 9
RESULTS — OPTIMUM BINDER CONTENT (OBC)
Marshall Mix Design Method — Trial Asphalt Contents: 4.0%, 4.5%, 5.0%, 5.5%, 6.0%
OPTIMUM BINDER CONTENT
5.0%
by weight of total mix Used for all 4 variants
OBC Determination Criteria
▸ Average of bitumen content at: (i) Maximum Marshall stability, (ii) Maximum bulk specific gravity, (iii) 4% design air voids
▸ Stability peaked at 5.0% then dropped — classic Marshall curve behavior
▸ Both local and imported binders yielded the same OBC of 5.0%
▸ At 5.0%: VMA, VFA, and unit weight all within RHD specification limits
Key Volumetric Equations
▸ Gmb = Wa / (Wssd – Ww) — Bulk Specific Gravity
▸ Va (%) = 100 × (Gmm – Gmb) / Gmm — Air Voids
▸ VMA (%) = 100 – (Gmb × Ps) / Gsb — Voids in Mineral Aggregate
▸ VFA (%) = (VMA – Va) / VMA × 100 — Voids Filled with Asphalt
9/16

## Slide 10
RESULTS — COMPARATIVE ANALYSIS OF MIXES
All Four Variants at 5.0% OBC
Mix-1
Local + Normal
Marshall Stability
1959 lbs (8.7 kN)
Flow
10.0 units
Air Voids
3.27%
VFA
78.20%
Unit Wt (pcf)
149.64
Mix-2
Imported + Normal
Marshall Stability
1119 lbs (5.0 kN)
Flow
17.0 units
Air Voids
4.90%
VFA
70.78%
Unit Wt (pcf)
146.52
⚠ LOWEST STABILITY
Mix-3
Local + 20% Cubical
Marshall Stability
2991 lbs (13.3 kN)
Flow
8.5 units
Air Voids
5.20%
VFA
68.86%
Unit Wt (pcf)
146.64
★ BEST PERFORMER
Mix-4
Imported + 20% Cubical
Marshall Stability
2070 lbs (9.2 kN)
Flow
12.0 units
Air Voids
2.59%
VFA
82.65%
Unit Wt (pcf)
150.07
10/16

## Slide 11
KEY FINDINGS & DISCUSSION
167%
Stability Improvement
Mix-3 vs Mix-2
50%
Deformation Reduction
Flow: 8.5 vs 17.0 units
13.3 kN
Highest Marshall Stability
Local + 20% Cubical
2.59%
Risk: Low Air Voids
Imported + Cubical (Mix-4)
Structural Performance
▸ Local ERL bitumen has lower penetration → stiffer mix → higher load capacity [8]
▸ Cubical aggregates interlock better, creating more internal friction [3, 5]
▸ Mix-3 combines both advantages: best binder + best aggregate shape
▸ Higher structural layer coefficient (a₁) → thinner pavement layers needed
▸ Less material per km of road → lower construction costs
Volumetric Concerns
▸ Mix-4 (Imported + Cubical): Air voids only 2.59%, VFA 82.65%
▸ In subtropical monsoon climate, this risks binder bleeding & plastic flow [2]
▸ Mix-3 (Local + Cubical): VMA 16.70%, Va 5.20% — balanced volumetrics
▸ Confirms binder-aggregate interaction is not additive — depends on the combination
▸ Imported bitumen softening point (41°C) too low for Bangladesh temperatures
11/16

## Slide 12
PAVEMENT THICKNESS & COST EFFECTIVENESS
AASHTO Structural Design Implications
Required Pavement Thickness Ranking
Mix-3: Local + Cubical
THINNEST — Highest a₁
Mix-1: Local + Normal
Moderate
Mix-4: Imported + Cubical
Moderate-High
Mix-2: Imported + Normal
THICKEST — Lowest a₁
Cost-Effectiveness Analysis
▸ Higher Marshall stability → Higher structural layer coefficient (a₁)
▸ Higher a₁ → Same SN achieved with THINNER asphalt layer
▸ Thinner layer = Less bituminous material per km of road
▸ Material savings offset costs of local refining & aggregate sorting
▸ Net effect: Lower lifecycle cost over the pavement's service life
▸ Mix-3 is the most cost-effective option for heavy-traffic pavements
12/16

## Slide 13
PROPOSED ROADMAP FOR COST-EFFECTIVE ROAD CONSTRUCTION
A Two-Level Strategy for Bangladesh
LEVEL 1 — Foundation (Subgrade Stabilization)
▸ Weak subgrade soils are common across Bangladesh
▸ Treat subgrade with lime and fly ash → raises CBR [7]
▸ Stronger subgrade → thinner base and sub-base layers
▸ Less aggregate material needed for foundation
▸ Proven effective in similar tropical conditions (Sood & Bansal, 2015)
LEVEL 2 — Surface (Optimized Bituminous Mix)
▸ Use local ERL bitumen (60/70 grade) — superior rheological properties
▸ Add ≥20% cubical aggregates in coarse fraction
▸ Marshall stability: 2991 lbs, Flow: 8.5 units
▸ Higher structural layer coefficient (a₁) per AASHTO 1993
▸ Thinner pavement layers → less material per km
Combined Effect: Stabilized foundation + Optimized surface = Same SN with thinner layers → Lower cost, higher durability
13/16

## Slide 14
CONCLUSIONS
1
Local ERL bitumen showed superior rheological properties — higher viscosity, consistent penetration grades, meeting all test requirements.
2
Mix-3 (Local + 20% Cubical) achieved the highest Marshall stability of 2991 lbs (13.3 kN) with flow of 8.5 units.
3
Imported bitumen + cubical aggregates (Mix-4) produced dangerously low air voids (2.59%) — risk of binder bleeding.
4
Local ERL bitumen + cubical aggregates provides both structural strength and volumetric stability.
5
Two-level roadmap proposed: subgrade stabilization (lime/fly ash) + optimized surface (ERL + cubical agg.).
6
Recommendations: RHD should add quality control for imported bitumen and aggregate shape sorting to specifications.
14/16

## Slide 15
FUTURE WORK
Expanding the Research Horizon — Next Steps for Comprehensive Pavement Evaluation
🔬
Indirect Tensile Strength (ITS) Testing
ASTM D6931 — Evaluate tensile loading resistance and fracture behavior of all mix combinations.
🌧️
Moisture Susceptibility & Climate Resistance
Retained stability tests (Marshall immersion) and TSR tests under Bangladesh's monsoon conditions.
🛞
Rutting & Fatigue Evaluation
Hamburg Wheel Tracking (AASHTO T 324) for rutting depth; Four-Point Bending Beam (AASHTO T 321) for fatigue life.
⚗️
Polymer Modified Bitumen (PMB)
Investigate 5% SBS polymer addition following LGED specs — potential for dramatic load-bearing and fatigue improvements.
♻️
Performance Enhancement of Imported Bitumen
Additives (SBS polymer, crumb rubber, waste plastics) to bring imported binder properties closer to local ERL standards.
15/16

## Slide 16
REFERENCES
[1] Werkineh, A.B. & Demissie, B.A. (2020). Assessment on the Performance of Pavement Structure Due to Subsurface Course Materials. Int. J. Adv. Multidiscip. Eng. Sci., 3(1), 8–15.
[2] Imran, U., Khurshid, M.B. & Khan, U. (2025). Developing a quality index for pavement construction and rehabilitation. Org. Tech. Mgmt. Constr., 17, 24–45.
[3] Teja, Y.P. & Krishna, K.H. (2020). Effect of Coarse Aggregates Shape Factors on Rutting Characteristics of Bituminous Mixtures. IJAEM, 2(3), 454–462.
[4] Khairandish, M.I. & Chopra, A. (2020). Influence of Size and Shape of Aggregate on the Mechanical Response of Bituminous Mixes: A Review. IRJET, 7(2).
[5] Sumanth, S., Suhas, R. & Mahendra, S.P. (2017). A Study on the Influence of Shape of Coarse Aggregates on Strength of Dense Bituminous Macadam. IJRTI, 2(9).
[6] Rajkumar, J.S.S., Vijayalakshmi, M.M. & Lakshmi, S. (2018). Experimental Investigation on Bituminous Mixes with MoRTH and Superpave Gradation. IJCIET, 9(12), 461–471.
[7] Sood, S. & Bansal, S. (2015). Evaluation of Construction Materials for Soil Stabilization in Road Making Industry. IJERT, 4(5), 404–410.
[8] Bagampadde, U., Isacsson, U. & Kiggundu, B.M. (2006). Impact of bitumen and aggregate composition on stripping in bituminous mixtures. Mat. Struct., 39, 303–315.
[9] Verma, P.K. & Khare, A. (2024). Study on effects of aggregate size, shape, and surface texture on the properties of bituminous mixtures. IJIERM, 11(6), 235–241.
16/16