# SPECIFIC GRAVITY OF BITUMINOUS MATERIAL

Data Collection

- = mass of pycnometer (plus stopper)

- = mass of pycnometer filled with water

- = mass of pycnometer partially filled with bitumen

- = mass of pycnometer + bitumen + water

Calculation:

Specific gravity = (C − A) / [(B − A) − (D − C)]

| Weight in gram | Pycnometer 01 ERL | Pycnometer 02 Cheap(low cost) | Pycnometer 03 |
| --- | --- | --- | --- |
| Mass of pycnometer (plus stopper) A | 101.5 | 101.5 |  |
| Mass of pycnometer filled with water B | 275.1 | 275.1 |  |
| Mass of pycnometer partially filled with bitumen C | 217.3 | 216.6 |  |
| Mass of pycnometer + bitumen + water D | 277.7 | 274.1 |  |
| Specific Gravity | 1.023 | 0.99 |  |

# PENETRATION OF BITUMINOUS MATERIAL

Data Collection

Initial dial gauge reading (mm)

Final dial gauge reading (mm)

Calculation:

Penetration = (Initial dial gauge reading − Final dial gauge reading) × 10 Data Table:

| Sample No. | Locally Produced Bitumen (ERL) | Imported Cheap Bitumen | 3 | 4 |
| --- | --- | --- | --- | --- |
| Initial dial gauge reading (mm) | 225 | 220 |  |  |
| Final dial gauge reading (mm) | 289 | 288 |  |  |
| Penetration (0.1 mm) | 64 =6.4mm | 68 =6.8mm |  |  |

Result:

Average Value (Penetration) = ________________

N.B.: The three penetration values obtained on the sample must agree within the following limits:

| Penetration | 0 to 49 | 50 to 149 | 150 to 249 | 250+ |
| --- | --- | --- | --- | --- |
| Maximum difference between highest and lowest determination | 2 | 4 | 6 | 8 |

BITUMEN SOFTENING POINT TEST (Ring & Ball)

Data Collection

| Sample No. | Time (min) | Temperature (°C) |
| --- | --- | --- |
| ERL- Locally Produced Bitumen | 13.67 | 52 |
| Imported Cheap Bitumen | 13.05 | 41 |

Average Value of Softening Point (°C) = ________________

Calculation:

The ring and ball softening point is simply the average of the two temperatures at which the bitumen just touches the bottom plate.

# FLASH POINT AND FIRE POINT TESTS OF BITUMEN

Data Collection

| Parameter | Value |
| --- | --- |
| Air Pressure (760mm of Hg) |  |
| Observed Flash Point (°C) |  |
| Observed Fire Point (°C) | Locally Produced Bitumen; Imported Cheap Bitumen. 255; 218. 312; 253. |

Calculation:

Air Pressure, P = ___760_____ mm Hg

Observed Flash and Fire points are in (°C)

Corrected flash or fire point = C + 0.03 × (760 − P)

** Corrected flash point = C + [0.03 × (760 − P)]

** Corrected fire point = C + [0.03 × (760 − P)]

Result:

At _760_______ mm Hg atmospheric pressure,

DUCTILITY TEST OF BITUMINOUS MATERIALS

| Sample name | ERL(locally produced Bitumen) | Cheap(imported cheap Bitumen) |
| --- | --- | --- |
| Initial Reading(cm) | 166 | 166 |
| Final Reading (cm) | 278 | 259 |
| Result (cm) | 112 | 91 |